## Slide 1
Renewable Energy Postgraduates Symposium (REPS)
By
Asanda Bede
Morphological and structural characterization of nano-sized carbon supported MoS2 as Pt-free CE materials for DSSCs application.
Supervisor: Prof. E. L. Meyer
Co-supervisor: Dr. R.T. Taziwa
Co-supervisor: Dr. D. Katwire
12 September 2018

## Slide 2: Outline
Introduction
Methodology
  Metal sulfide synthesis
Results and discussions
  SEM
  HRTEM
  XRD
  Raman
  FTIR
  CV, CD and EIS
References
Acknowledgements
12 September 2018

## Slide 3
High demand in energy due to an increasing population.
Coal fired power plants produce most of the electricity consumed in SA.
Silicon-based technology
-Widespread
-High Efficiency
-Expensive to manufacture
Introduction
Dye-sensitized (“nano”)
-Newer,
- less proven
-Inexpensive to manufacture
-Flexible

## Slide 4
Due to HIGH COST, HIGH DEMAND, LIMITED RESERVES.
Not appropriate for the redox species like Co3+/Co2+ and polysulfide electrolytes.
40% total cost of Manufacturing DSSC.
New alternative materials / Pt FREE Catalysts need to be explored.
Introduction

## Slide 5: Experimental
MoS2 samples (black precipitate), Multi-walled carbon nanotubes, and polyvinylidene fluoride (weigh ratio 8: 1: 1), were dissolved in N-methyl-2-pyrrolidinone.
Subsequently, the as-prepared slurry was paint brush on Ni foam at area of 1cm2 . The coated CEs were dried at 700C for overnight in an oven.
12 September 2018
MoS2 (mg) | MWCNTS (mg) | PVF (mg) | Mole Ratio
240 | 30 | 30 | 8:1:1
210 | 60 | 30 | 7:2:1
180 | 90 | 30 | 6:3:1
150 | 120 | 30 | 5:4:1
120 | 150 | 130 | 4:5:1
90 | 180 | 30 | 3:6:1
60 | 210 | 30 | 2:7:1
30 | 240 | 30 | 8:1:1

## Slide 6: Experimental
SEM.
Raman Spectroscopy.
XRD.
FTIR

## Slide 7
Results: SEM
SEM reveals Spherical MoS2 NPs produced via hydrothermal method.
Also, reveals the distribution of MWCNTs on MoS2

## Slide 8
Results: HRTEM
HRTEM were employed to elucidate the structures of MoS2 and MoS2/MWCNTs

## Slide 9
Results: XRD
(002) peak of MoS2 have shifted from 15. 40 to higher degree at 18.30, denoting an outstanding interlayer expansion.
Major detectable peaks could be indexed to 1T-MoS2.

## Slide 10
Results: Raman
Two Raman modes detected Eg and Ag.
D, G and 2D’ modes were also detected.

## Slide 11
Intense absorption bands at 457 cm-1, 1126 cm-1, 1409cm-1, 1696 cm-1
Results: FTIR

## Slide 12
Results: Electrochemistry
Figure (a) reveals CV curve for MoS2 electrode at scan rates of 5, 10, 20, 50 and 100 mVs−1.
The shape of these CV curves show no obvious change with increase in scan rate from 5 mVs−1 to 100 mVs−1

## Slide 13
SEM ANALYSIS
Morphological analysis of MoS2 and
MoS2/MWCNTs were successfully
evaluated using SEM
Conclusion

## Slide 14
Conclusion
XRD AND RAMAN ANALYSIS
Structural analysis of MoS2 and
MoS2/MWCNTs were successfully
evaluated using XRD and Raman.

## Slide 15
Conclusion
FTIR ANALYSIS
FTIR confirmed that S is
bonded to Mo.

## Slide 16
Recommendations
Perform Electrochemical characterization of
MoS2/MWCNTs CE.
As well as elemental analysis.
Evaluate the DSSC employing MoS2 and
MoS2 /MWCNTs.
Investigate the effect of doping on the
performance of the DSSC.

## Slide 17: References
Won J.L., Easwaramoorthi R., Dong Y.L., Jae S.S., “Efficient dye-sensitized solar cells with catalytic multiwall carbon nanotube counter electrodes,” ACS applied materials & interfaces 2009, 6, 1145–1149.
“Dye Solar Cells for Real–The assembly guide for Making Your Own Cells”, Solaronix.
O’Regan B, Gratzel M. A low-cost, high-efficiency solar cell based on dye-sensitized colloidal TiO2 films. Nature 1991; 353, 37–40.
Yu H., Zhang S.Q., Zhao H.J., Will G., Liu P.R., An Efficient and Low-Cost TiO2 Compact Layer for Performance Improvement of Dye-Sensitized Solar Cells, Electrochim. 2009, 54, 1319.
Park K.H., Dhayal M., High Efficiency Solar Cell Based on Dye Sensitized Plasma Treated Nano-Structured TiO2 Films, Electrochem. Commun.2009, 11, 75–79.
Fang X.M., Ma T.L., Guan G.Q., Akiyama M., Kida T., Abe E., Effect of The Thickness of The Pt Film Coated on A Counter Electrode on The Performance of A Dye-Sensitized Solar Cell, J. Electroanal. Chem. 2004, 570, 257–263.
Fang X.M., Ma T.L., Guan G.Q., Akiyama M., Abe E., Performances Characteristics of Dye-Sensitized Solar Cells Based on Counter Electrodes with Pt Films of Different Thickness, J. Photochem. Photobiol.2004, 164, 179–182.
12 September 2018

## Slide 18: Acknowledgements
My supervisors.
Fort Hare Institute of Technology (FHIT).
RENEWABLE AND SUSTAINABLE ENERGY (NRF).
12 September 2018

## Slide 19
THANK YOU ALL
12 September 2018